## Slide 2: Root canal filling

## Slide 10
Lentulo
Spreader

## Slide 11
Plugger - compactor

## Slide 12: Root canal filling
Guttapercha
Sealer

## Slide 13: Root canal filling

## Slide 14: Root canal filling
  Good coronal,
  Middle
  Apical seal.
1
2
3
Quality guidelines for endodontic treatment, European Society of of Endodontology (ESE), 1994

## Slide 15: Root canal fillings
Sealers
Cones
Guttapercha
Resilon
Silver/titanium
Pasts
Zinkoxid eugenol
Polyketons
Epoxy resins
Glasionomers
Calcium
hydroxide
Silicons
Composits/ adhesives

## Slide 16: Ideal root canal filling (Grossman 1988)
Easy mixing
Sufficient working time
Good seal
X- ray contrast
Easy removal
No shrinkage
Long term volume stability
No bacterial growing
No permeability for fluids
Biocompatibility
No staining

## Slide 17: Classification of root canal fillings
Solid
Semisolid
Pastes

## Slide 18: Guttapercha
Dried juice of the Taban tree (Isonandra percha)
(gutta)
1,4 - polyisoprene
Crystallin structure (60%)
Brittle

## Slide 19: Guttapercha
Beta phase
Alpha phase 42 – 49 °C
plastic
Gamma phase 56 – 62° (amorfní)
Cooling process
very slowly (less than 0,5°C) – alpha phase
normal cooling– beta phase

## Slide 20: Composition of guttapercha materials in endodontic
Guttapercha 19% – 22%
Zinc oxide 59 - 79%
Heavy metal salts 1% - 7%
Wax or resin 1% - 4%

## Slide 21: Resilon (Pentron)
Thermoplastic synthetic polymer
Points or material for injection
Composition:
Polyester polymers
Bioactive glass
Radioopaque fillers (bismuthum oxichlorid a and
baryum sulphate)

## Slide 22: Silver or titanium cones
No good seal
Silver cones - corrosion

## Slide 23: Sealery
Chemically curing plastic materiáls
Good adhesion to root canal walls as well as solid cones
X- ray contrast
Biocompatibility

## Slide 24: Sealers
Zinc Oxide-Eugenol
Chloropercha
Calciumhydroxide
Resins
Glasionomer
Silicone

## Slide 25: Sealers
Importance
Filling of the spaces between the solid cones
Seal of the root canal filling

## Slide 26: Zinc - Oxid Eugenol
Powder:
Zinc oxide
Liquid:
Eugenol
Acidic resins
Good adhesivity, antimikrobial effect, cytotoxic. resorbable)

## Slide 27: Zink Oxid Eugenol sealers
Pulp Canal Sealer (Kerr, USA))
Tubuli- Seal (Kerr, USA)
Caryosan (Spofa Dental, ČR)

## Slide 28: Chloropercha
Powder
Canadian balsam
Resins
Guttapercha
Zinc oxide
Liquid:
Chloroform
Resins

## Slide 29: Chloroperča
Vlastnosti:
Good adhesivity
Shrinkage
Toxicity

## Slide 30: Calciumhydroxide sealers
Base ( powder)
Calcium hydroxide
Zinc oxide
Other components and vehicula

## Slide 31: Kalciumhydroxidové sealery
Catalystr (paste)
Zinc stearat
Titanium dioxide
Baryum sulphate
or
Eugenol,. Eukalypt
others

## Slide 32: Kalciumhydroxide sealers
Increase of the healig potential of periapical tissues
Antibacterial effect
Easy manipulation
But!
Resorbable if not homogeneus
Not suitable for the single cone technique

## Slide 33: Resins
Rezorcin formaldehyd
Epoxide
Polyketone
Metacrylate

## Slide 34: Rezorcin – formaldehyd resins
Toxicity
N2, Endomethason, Riebler´s paste, Foredent

## Slide 35: Epoxide resin
Base (powder, paste)
Bismuth oxid
Titanium dioxide
Hexametylentetramine
(Silver)
Catalyst (liquide, paste)
Bisphenoldiglycidylether

## Slide 36: Epoxid resin (advantages)
Long working time
Hydrophilic (good penetration)
Good adhesion to the root canal walls
Volume stability
No dissolution
Antibacterial

## Slide 37: Epoxidové pryskyřice (disadvantages)
Difficult removal
Staining
Initiatiory roxicity
No suitable for the single cone technique !

## Slide 38: Polyketone
Base
Zinc oxide
Bismuth phosphate
Hexametylentetramine
Liquid
Bisphenolglycidylether and other components

## Slide 39: Polyketon resins
Advantages
Good adhesion
No contraction
No dissolution
Disadvantages
High stickness
Not removable
Products: Diaket, Diaket A (3M ESPE)

## Slide 40: Methacrylate resins
Endo ReZ (Ultradent) – UDMA
For injection – single cone technique
Epiphany (Pentron)
Bis- GMA, etoxy bif- GMA, hydrophilic bifunctional
methacrylates
Calcium hydroxide, baryum sulphate, baryum glass
silica.
Sealer in combination with Resilon

## Slide 41: Glasionomer sealers
Base (powder)
Aluminium silicate glass
Liquid
Polyacrylic acid, polymaleic acid, tartaric acid

## Slide 42: Glasionomer sealers (Advantages and disadvantages)
Advantages:
Curing under wett conditions, chemical bonding to hard
dental tissues, no staining
Disadvantages
Short working time, difficult removal,
porous
Products
Ketac Endo (3M ESPE), Endion (VOCO)

## Slide 43: Silicon based sealers
Polyvinylsiloxane (ev. in mixture with powdered
guttapercha
Biocompatibility
Hydrofillic
Further investigation desirable.

## Slide 44: Root canal filling
A cone inside the sealer – core material
Guttapercha
Resilon
Silver cones
Custom cones

## Slide 45: Root canal filling
Guttapercha
Trans isomer of polyisoprene
2 crystalline forms (alpha, beta)
Beta – room temperature
Alpha after heating
Various process of cooling
Extremly slow cooling: Aplha phase recrystalize.
65°.
Less shrinkage, more dimensionally stable

## Slide 46: Root canal filling
Guttapercha
20% gutta-percha
65% zink oxide
10% radioopacifiers
5% plasticizers

## Slide 47: Root canal filling
Guttapercha
Cones: conventional and standardized sizes
Conventional: dimension of the tip and body
Standardized cones are designed to match the
taper of the instrument.

## Slide 48: Root canal fillings - forms
Points (Cones)
Materials for injection
Plastic materials

## Slide 49: Instruments
Lentulo
Compactors
Compactors - carriers
Others

## Slide 50
Lentulo
delivers pastes
1,5 – 2 mm ahead
at most for Ca (OH)2

## Slide 51
Spreader
Compactors
Pointed
Vertical introduction
Lateral condensation
technique

## Slide 52
Plugger
Not pointed
Vertical introduction
Vertical condensatuion
- compaction
Compactors

## Slide 53: Filling techniques
Cold
Warm

## Slide 54: Single cone technique
Easy
Fast
Good control of WL
Standard round preparation – risk of leakage
Wesselink, P.: Root filling techniques, Textbook of Endodontology; p. 286-299, Blackwell Munksgaard 2003, Oxford

## Slide 55
Shrinkage, difficult removal
Paste only

## Slide 57: Lateral condensation Lateral compaction
Standard cold technique
Wesselink, P.: Root filling techniques, Textbook of Endodontology; p. 286-299, Blackwell Munksgaard 2003, Oxford

## Slide 59: Warm lateral condensation

## Slide 61
Centrální čep
Laterální kondenzace

## Slide 62: Vertical condensation

## Slide 64: Injection
Rychlá technika
Možná extruze sealeru
Teplo

## Slide 65
Perfektní hermetický uzávěr i u kanálků s nepravidelným tvarem

## Slide 66
Fáze plnění 2. Backfill
BeeFillem hermeticky uzavřeme a zaplníme zbývající část kanálku kulatého i oválného a uzavřeme postranní ramifikace ve vrchních částech kanálku.