Sequences of operations

Complete denture

The transfer of occlusal forces – mucosal only.

Tissue supported (born) denture.

Made usually of the acrylic resin - methylmetacrylate.

Sequence of operation

- I. phase in dental office

- Taking impression (alginate the best choice)

- I. phase  in dental lab

Pouring: gypsum model

Fabrication of the indivindiual impression tray – shelack or acrylic

II. phase in dental office

Ranging with the special low – fusing wax (the functional tray).This procedure is

done in the patient. The tray must be accurate without any excess, the wax

makes the tray more precise, patient moves with his/her

lips and cheeks – the function is important for the impresiion of details.

After this procedure the tray is called the functional tray

The impression after that is called the functional impression.

During this procedure patient is moving with his/her

lips and cheeks again. The most suitable material is

the zinkoxideugenol paste – a special impression material for edentulous jaws.

- II. phase in dental lab

Ranging of the impression with the wax

The border of the functional impression.

must be protected using the wax strip. After that. The bite template is

fabricated  as usually using  shellack or acrylic for the base, the wall is made of  wax. The width of the wax wall  in frontal area is around 8 mm, in posterior area 10 mm.

III. phase in dental office

Registration of the intermaxillary relationship.

The procedure consist

of two steps

1. Vertical relationship. The neck of the patient

is perpendicular to the horizontal plane. The occlusal

plane must be parallel to the bipupilar line in the frontal area and to

nasoauriculal line in the posterior area. The wax walls must be

plain cut, the height is according to the free position

of the mandible.  After that the height is

reduced – 2 mm. This is a vertical relationship.

2. Horizontal relationship

The head of the patient

is bent backward and he/she swallows. This can halp us to find the horizontal

relationship. After these procedures the wax walls must be

put together (with paperclips or wax or other material). Ahter the bite registration

in the same phase the colour of teeth is choosen using the colour card (colour shade guide).

III. phase in dental lab

The wax pattern of the denture is made

This is made of wax – base and acrylic teeth are built in it.

according to the registrate using the articulator or occludor.

IV. phase in dental office

The wax pattern of the denture is tried in the patient, the occlusion, aesthetic and fonation are checked.

IV. phase in dental office

The wax pattern is flasked into a four parts flask using gypsum

The teeth are insulated with a special silicone material.

The flask is closed and filled with the gypsum completely.

After the hardening of the gypsum  the flask is opened and the wax removed

The wax is removed using hot water. A thin tin foil is put

on some places, esp.  on palatal suture in order

to unload them. The insulating  agent based on alginate is used.

The flask is filled with the resin dought (mixed of powder and liquid), closed and put into a special cleap.

The resin is polymerized

using the 2,5 hours

polymerization

Schema:

1. During 1 hour reach

the temperature 70°C,

2. 30min interrupt heating

3. During further 30 min increase

the temperature – reach 100°C

4. 30 min stay on 100°C.

After that let the flask cool slowly.

The denture is taken out finished and polished

using special burs, grinding and polishing pastes.

V. phase in dental office

The denture is given over to the patient and the patient is informed how to use it.