## Slide 1: Restorative dentistry 3rd year Lecture 1
L. Roubalíková

## Slide 2: Preparation of dental caries (cavity preparation)
Instrumental treatment that removes dental caries
The rest of the tooth must be restorable with filling materials
The rest of the tooth as well as the filling must be resistant against occlusal forces
The risk of secondary caries must be minimized

## Slide 3: Step by step procedure
Acces to the cavity
Preparation of cavosurface margin and
Extention for prevention
Retention of the filling
Resistance of the restored tooth
Excavation of carious dentin
Finishing of the walls
Final control (light, mirror, magnification)

## Slide 4: Basic rules
Acces to the cavity
Preparation through the hard dental tissues
Removal the undermined enamel
Separation of teeth
Separation or removal of gingiva

## Slide 9
Old filling is being removed

## Slide 11: Basic rules
Preparation of cavity borders and extention
for prevention (Cavosurface margin)
Depends on
Dental material
Oral hygiene
Precautions of secondary caries

## Slide 12: Basic rules
Retention of the filling
Precautions of its lost
Macromechanical retention
Micromechanical retention
Chemical retention

## Slide 13: Basic rules
Resistance of the restored tooth
Against occlusal and other forces
Depends on
Material
Individual occlusal forces

## Slide 14: Basic rules
Excavation of carious dentin
Necessary (risk of recurrent caries)
Ball shaped (spheric) bur - slow speed (3000 rpm)
or
Excavator (hand instrument)

## Slide 15: Basic rules
Finishing of the walls
Depends on the kind of material
Bevel or without bevel
Fine diamond bur

## Slide 16: Basic rules
Final control
Direct or indirect view
Good illumination
Magnification

## Slide 17: Preparation
Hand
Excavator, cleaver
Power driven
Burs, diamonds

## Slide 18: Chisel – for enamel Cleaver

## Slide 19: Chisel for enamel

## Slide 20: Excavator

## Slide 21: Instruments for cavity preparation
Power driven (powered) instruments for cutting
Rotary instruments
Comon design characteristics
lenka.roubalikova@tiscali.cz
shank
neck
head

## Slide 22: Cutting instruments - burs
Steel
Tungsten carbide

## Slide 23: Cutting instruments – burs head shapes
Round (ball shaped)

## Slide 24: Cutting instruments – burs head shapes
Fissure with flat end
Fissure with pointed end
Straight or tapered form

## Slide 25: Cutting instruments – burs head shapes
Pear

## Slide 26: Cutting instruments – burs head shapes
Inverted conus

## Slide 27: Cutting instruments – diamonds
Extra coarse – black
Coarse – green
Standard – blue or without any marker
Fine - red
Extra fine - yellow
Ultrafine - white

## Slide 28: Cutting instruments – diamonds head shape
Ball, pear, cylinder,taper,flame, torpedo, lens and others…..

## Slide 29: Hazards with cutting instruments
Pulpal precautions
Soft tissue precautions
Eye precautions
Ear precautions
Inhalation precautions

## Slide 30: Filling materials
Temporary
Definitive, permanent

## Slide 31: Temporary filling materials
Zinkoxidsulphate cement and one
component derivates
Ziknoxidphosphate cement
Zinkoxideugenol cement
Polymer based materials
Guttapercha

## Slide 32: Permanent filling materials
Amalgam
Composites
Glasionomers

## Slide 33: Amalgam

## Slide 34: Amalgam
Metal-like restorative material composed of
silver-tin-copper alloy and mercury.

## Slide 35: Types of amalgam restorative materials
Low – Copper Amalgam (5% or less copper)
Composition – wt%
Silver 63 - 70 %
Tin 26 – 28 %
Copper 2 - 5%
Zinc 0 - 2%

## Slide 36: Types of amalgam restorative materials
High – Copper Amalgam (13% - 30%)
copper
Composition – wt%
Silver 40 - 70 %
Tin 26 – 30 %
Copper 2 - 30%
Zinc 0 - 2%

## Slide 37: Particles of the alloy
Irregulary shaped (filings - lathe cut)
Microsphers
Combination of the two.

## Slide 38: Particles shape
High – Copper Amalgam
Microsphers of the same composition
(unicompositional)
Mixture of irregular and spherical particles of
different or the same composition (admixed)

## Slide 39: Production of irregular particles
Metal ingrediences heated, protected from
oxidation, melted and poured into a mold to
form an ingot.
Phases of the alloy: (intermetallic
compounds)
Ag3Sn - g
Cu3Sn - e
Cu6Sn5 - h
Ag4Sn - b

## Slide 40: Production of irregular particles
Ingot cooled slowly
Ingot heated at 400°C (6 – 8 hours)
(homogeneous distribution of Ag3Sn)
Ingot cut on the lathe, particles passed trough a fine sieve
and ball milled to form the proper particle size.
Aging of particles (60 - 100°C, 6 – 8 hours)
Particle size: 60 – 120 mm in length
10 – 70 mm in width
10 – 35 mm in thickness

## Slide 41: Production of irregular particles
Molten alloy is spraying into water under
high pressue
Irregulary shaped high-copper particles

## Slide 42: Production of spherical particles
Molten alloy is spraying under
high pressue of inert gas through a fine
crack in a crucible into a large chamber
Diameter of the spheres: 2 – 43mm

## Slide 43: Amalgamation processes
Metal alloy is mixed with pure mercury
Trituration

## Slide 44: Amalgamation processes
Hg
Sn
Sn
Sn
Sn
Sn
Ag
Ag
Ag
Ag
Ag
Cu
Cu
Cu
Cu
Cu
Ag3Sn – g
Cu3Sn – e
Intermetallic compounds

## Slide 45: Amalgamation processes
Sn
Sn
Sn
Sn
Sn
Ag
Ag
Ag
Ag
Ag
Cu
Cu
Cu
Cu
Cu
Ag3Sn – g
Cu3Sn – e
Cu6Sn5 - h
Sn7Hg – g2
Ag2Hg3 – g1
High copper amalgam – copper dissolved in mercury has high reaction afinity
to tin that is also dissolved in mercury. It reacts with tin in gamma2 phase
and eta phase comes into existence.
The gamma 2 phase disappears.

## Slide 46: Setting of low copper amalgam
Principle of setting is crystallization
Structure of the amalgam filling
Ag-Hg: gamma 1
Sn-Hg: gamma 2
Gamma phase (Ag-Sn) does not dissolve
completely – remains in the structure
These phases crystallized – become hard

## Slide 47: Risks of the gamma 2 phase
Non stable
Tin is released due to electrogalvanism in oral cavity and mercury from this phase reacts with remaining gamma phase.
This is external electrochemical corrosion.
Low copper amalgam has worse mechanical and corrosion resistance than high copper amalgam

## Slide 48: High copper amalgam
Content of copper increased: 12 – 13%
(Less tin)
Or up to 25% ( Less tin and silver)
Better mechanical and corrosion resistance

## Slide 49: Amalgamation processes
Sn
Sn
Sn
Sn
Sn
Ag
Ag
Ag
Ag
Ag
Cu
Cu
Cu
Cu
Cu
Ag3Sn – g
Cu3Sn – e
Cu6Sn5 - h
Sn7Hg – g2
Ag2Hg3 – g1
High copper amalgam
g2 phase disappears or does not occur
depending on the content of copper
Gamma two disapears or it does not occur when content of copper is high

## Slide 50: Amalgam - properties

## Slide 51: Amalgam
Wear and pressure resistance (2mm thickness ast least)- brittleness
Easy handling
Low price
Thermal and electrical conductivity
Corrosion
Bad aesthetics
Flow (deformation of not completely set amalgam if the filling is loaded)
Creep – completely set amalgam can be deformed due to bite forces. The filimng is principly hammered.

## Slide 52: Biocompatibility
More than 160 years, more than 200 milions Ag fillings every year in USA.
Allergy rare
Precautions in children and in pregnancy.
AMALGAM IS STILL A MATERIAL OF CHOICE

## Slide 53: Toxicity
Organic compounds
Vapours, aerosol
Precautions
Ventilation
Rests of amalgam in water
Amalgam separators
Dangerous waste (180 110)

## Slide 54: Amalgam indications
Posterior area
I. a II. class : moderate or large cavities,
V. class
Other factores for consideration
When oral hygiene is not excellent
When patient wants low cost filling.

## Slide 55: Indications and contraindications of amalgam
Indications
Moderate and large cavities in posterior area (class I., II. V)
Contraindications
Fillings in frontal area
Pregnancy, children till the age of 15
Allergy
Other factores for consideration
When oral hygiene is not excellent
When patient wants low cost filling.

## Slide 56: Mixing of amalgam
Hand mixing (obsolete)
Power driven trituration
Amalgamators

## Slide 58
Cup
Amalgam gun
Condensor

## Slide 59
Amalgam gun
Crucible (cup)

## Slide 60
Power driven condensation
handpiece
condensor

## Slide 62: Instruments
Preparation instruments
Filling instruments
Carvers
Burnishers

## Slide 63: Instruments
Preparation instruments - power driven
Burs
Diamonds

## Slide 64: Instruments
Preparation instruments - hand
Chisel
Excavator

## Slide 65
Amalgam carrier

## Slide 66: Amalgam carrier

## Slide 67: Instruments
Filling instruments condensors and spatulas

## Slide 68
Condensor with flat front

## Slide 69: Condensor with flat front

## Slide 70: Condensor and burnisher - spatula combined

## Slide 71
Power driven condensor
Special handpiece

## Slide 72: Burnisher - spatula Angular- trough edge trough face

## Slide 73: Burnisher – spatula, angular three face

## Slide 74: Instruments
Burnishers

## Slide 75: Ball condensor – used as a burnisher at most