## Slide 1: C6730 Fázové rovnováhy
P08 SW a termodynamické databáze pro výpočty FR
Doc. Jiří Sopoušek

## Slide 2: Osnova dnešní přednášky
Algoritmus výpočtu FR
Assessment
SW pro metodu CALPHAD a Termodynamické databáze
Diskuse
Notes: Dohodnout termín a místo konání přednášky, seznam posluchačů (vč. jejich zaměření)

## Slide 3: Algoritmus výpočtz FR metodou CALPHAD

## Slide 4: CALPHAD metoda
Termodynamická databáze
Gibbsova energie fází jako funkce p, T a složení
Řešení fázové rovnováhy (složení koexistujících fází,…)
Fázový diagram soustavy




Celkové složení soustavy, T,p, vazné podmínky (zákon zachování hmoty, stechiometrie, elektroneutrality)
Minimalizace celkové Gibbsovy energie soustavy
Gibbsova energie fází jako funkce p, T a složení
Gibbsova všech energie fází jako funkce p, T a složení

Termodynamické parametry (experimentálně dosažitelné z termodynamických měření, získatelné z fázových dat, „ab-initio výpočet“ )
Termodynamické modely fáze
Podmíněná minimalizace účelové funkce mnoha proměnných

## Slide 5: Algoritmus assessmentu FD

## Slide 6: pokračování

## Slide 7: CALPHAD assessment
http://www.flyhy.eu/science_wp3.html

## Slide 8: SW - DATABASES IN CHEMICAL THERMODYNAMICS
Jméno | Původ | Obsah | Přístup
Thermo-Calc | Royal Institute of Technology (Swe) | Software for thermodynamic and phase diagram calculations, specially designed for systems with strongly non-ideal phases. Assessment. | Pc and workstation, commertial
Pandat | CompuTherm LLC (JP) | Phase diagrams and related thermodynamic calculations. Celkova G energie | Commercial.
F*A*C*T | École Polytechnique de Montréal (FR) | Integrated thermochemical database which couples software with thermodynamic data. | online, PC and web. Commertila
MT-data | NPL (UK) | Databank system for thermochemical data | PC-disks, commercial

## Slide 9: Pokračování
Jméno | Původ | Obsah | Přístup
Thermocomp (Thermodoc) Gemini | THERMODATA | Thermodynamic properties of elements and substances in inorganic chemistry, and their reactions. (Bibliographic references pertaining to the thermodynamic properties of elements, stoichiometric substances, alloys and non-stoichiometric phases of interest to dry mineral chemistry). | Transpac, Internet.
Thermophysical and Thermochemical Property Database | JICST. factual databases (JOIS-F) | thermophysical and related data for inorganic and low molecular weight compounds and up to 3-component systems. | planned for WWW, subscript. Note: this service is temporary down

## Slide 10: Další zdroje informací o FD
http://www.crct.polymtl.ca/thermo_databases.html
VLXE (polymery) free: http://www.vlxe.com
Diagramy: ASM : ttp://www.asminternational.org/asmenterprise/apd/default.aspx
http://www1.asminternational.org/AsmEnterprise/APD/
STGE: http://www.crct.polymtl.ca/sgte/index.php
Diagramy (JP) NIMS: http://www.nims.go.jp/cmsc/pst/database/periodic.htm
Assessment
Kniha:
http://www.springerlink.com/content/100270622k03v066/

## Slide 11: Diskuse

## Slide 12
fcc+MX
bcc+
carbid M23+
Carbonitrid MX
Fcc+M7+MX
1
2
fcc+ MX+M23
3
bcc+M7+MX
Řez FD žárupevné oceli P91:
Fe-9%Cr-0,1%Ni-
0,96%Mo-0,3%V-
0,045%N-0,1%C
(Mn, Si, P, S, Nb)
1 bcc+MX+M23+M6
2 bcc+fcc+MX
3 bcc+M23+M7+MX
