## Slide 1: FUNDAMENTALS OF METAL ALLOYS, EQUILIBRIUM DIAGRAMS
Chapter 4

## Slide 2: 4.2 What is a Phase?
Phase is a form of material having characteristic structure and properties.
More precisely: form of material with identifiable composition (chemistry), definable structure, and distinctive boundaries (interfaces) which separate it from other phases.

## Slide 3: 4.2 Phases
Phase can be continuous (air in the room) or discontinuous (salt grains in the shaker).
Gas, liquid or solid.
Pure substance or solution ( uniform structure throughout).

## Slide 4: 4.3 Equilibrium Phase Diagrams
Graphic mapping of the natural tendencies of a material or a material system (equilibrium for all possible conditions).
Primary variables: temperature, pressure and composition.
P-T diagram (the simplest).

## Slide 5: 4.3 Temperature-Composition Diagrams
Engineering processes conducted at atmospheric pressure (P/T variations).
The most common: temperature-composition phase diagrams.

## Slide 6: 4.3 Cooling Curves
Cooling curves for NaCl-H20 combinations:

## Slide 7: 4.3 Cooling Curves
Partial equilibrium diagram of NaCl-H20 system

## Slide 8: 4.3 Solubility
Solubility limits.
Degree of solubility determines properties.
I-Two metals completely soluble in each other.
II- Two metals soluble in liquid state and insoluble in solid state.
III-Two metals soluble in liquid state and partially soluble in solid state.

## Slide 9: 4.3 Complete Solubility
Copper-Nickel equilibrium diagram

## Slide 10: 4.3 Partial Solid Solubility
Degree of solubility depends on temperature
At max. solubility, 183 C: lead holds up to 19.2 wt% tin in a single phase solution, and tin holds up to 2.5wt% lead and still be a single phase.

## Slide 11: 4.3 Utilization of Diagrams

## Slide 12: 4.3 Example problem

## Slide 13: 4.3 Utilization of Diagrams
The phases present.
Composition of each phase ( single phase region or two phase region).
In two phase region a tie-line should be constructed.
The amount of each phase present: lever-law calculation using a tie-line.

## Slide 14: 4.3 Three Phase Reactions

## Slide 15: 4.4 Iron-Carbon Equilibrium Diagram

## Slide 17: 4.4 Iron-Carbon Equilibrium Diagram
,(present only at extreme temperatures)
Austenite, (FCC, high formability, high solubility of C, over 2%C can be dissolved in it, most of heat treatments begin with this single phase).
Ferrite, BCC, stable form of iron below 912 deg.C, only up to 0.02 wt% C in solid solution and leads to two phase mixture in most of steels.
Cementite (iron-carbide), stoichiometric intermetalic compound, hard, brittle, exact melting point unknown.
Currie point (770 deg. C), atomic level nonmagnetic-to-magnetic transition.

## Slide 18: 4.4 Three Phase Reactions
Peritectic, at 1495 deg.C, with low wt% C alloys (almost no engineering importance).
Eutectic, at 1148 deg.C, with 4.3wt% C, hapends to all alloys of more than 2.11wt% C and they are called cast irons.
Eutectoid, at 727 deg.C with eutectoid composition of 0.77wt% C, alloys bellow 2.11%C miss the eutectic reaction to create two-phase mixture. They are steels.

## Slide 19: 4.5 Steels

## Slide 20: 4.5 Eutectoid Steel
At 0.77%C by cooling from austenite (FCC) changes to BCC-ferrite (max 0.02%C) and excess C forms intermetalic cementite.
Chemical crystalline solid separation gives fine mixture of ferrite and cementite. Perlite (right), 1000X.

## Slide 21: 4.5 Hypoeutectoid Steel
With less than 0.77%C from austenite by cooling transformation leads to growth of low-C ferrite growth. At 727deg.C austenite transforms in to pearlite.
Mixture of proeutectoid ferrite (white) and regions of pearlite forms.
Magnification 500X.

## Slide 22: 4.5 Hypereutectoid Steel
With more than 0.77%C, from austenite transformation leads to proeutectoid primary cementite and secondary ferrite. At 727 deg.C austenite changes to pearlite.
Structure of primary cementite and pearlite forms.
Magnification 500X.

## Slide 23: 4.6 Cast Irons
Iron-Carbon alloys of 2.11%C or more are cast irons.
Typical composition: 2.0-4.0%C,0.5-3.0% Si, less than 1.0% Mn and less than 0.2% S.
Si-substitutes partially for C and promotes formation of graphite as the carbon rich component instead Fe3C.

## Slide 24: 4.6 Gray Cast Iron
Composes of: 2.5-4.0%C, 1.0-3.0%Si and 0.4-1.0% Mn.
Microstructure: 3-D graphite flakes formed during eutectic reaction. They have pointed edges to act as voids and crack initiation sites.
Sold by class (class 20 has min. tensile strength of 20,000 psi is a high C-equivalent metal in ferrite matrix ). Class 40 would have pearlite matrix.

## Slide 25: 4.6 Gray Cast Iron
Properties: excellent compressive strength, excellent machinability, good resistance to adhesive wear (self lubrication due to graphite flakes), outstanding damping capacity ( graphite flakes absorb transmitted energy), good corrosion resistance and it has good fluidity needed for casting operations.
It is widely used, especially for large equipment parts subjected to compressive loads and vibrations.

## Slide 26: 4.6 White Cast Iron
Composes of: 1.8-3.6%C, 0.5-1.9%Si and 0.25-0.8%Mn.
All of its carbon is in the form of iron-carbide (Fe3C). It is called white because of distinctive white fracture surface.
It is very hard and brittle (a lot of Fe3C).
It is used where a high wear resistance is dominant requirement (coupled hard martensite matrix and iron-carbide). Thin coatings over steel (mill rolls).

## Slide 27: 4.6 Malleable Cast Iron
Formed by extensive heat treatment around 900 degC, Fe3C will dissociate and form irregular shaped graphite nodules. Rapid cooling restricts production amount to up to 5 kg. Less voids and notches.
Ferritic MCI: 10% EL,35 ksi yield strength, 50 ksi tensile strength. Excellent impact strength, good corrosion resistance and good machinability.

## Slide 28: 4.6 Pearlitic Malleable Cast Iron
Pearlitic MCI: by rapid cooling through eutectic transformation of austenite to pearlite or martensite matrix.
Composition: 1-4% EL, 45-85 ksi yield strength, 65-105 ksi tensile strength. Not as machinable as ferritic malleable cast iron.

## Slide 29: Ductile Cast Iron
Without a heat treatment by addition of ferrosilicon (MgFeSi) formation of smooth spheres (nodules) of graphite is promoted.
Properties: 2-18% EL, 40-90 ksi yield strength, 60-120 ksi tensile strength.
Attractive engineering material due to: good ductility, high strength, toughness, wear resistance, machinability and low melting point castability.

## Slide 30: 4.6 Malleable Cast Iron
Ductile iron with ferrite matrix (top) and pearlite matrix (bottom) at 500X.
Spheroidal shape of the graphite nodule is achieved in each case.

## Slide 31: Microstructure
Globular cast iron

## Slide 32: BCC Unit Cell

## Slide 33: FCC Unit Cell