## Slide 1: Heterogeneous catalysis (C9981)
Kinetics
Mechanisms of catalytic reactions
Diffusional limitations on heterogeneous catalysts

## Slide 2: Definition
Catalyst is…
  A substance that speeds up a chemical reaction
  Without being consumed or changed
+ CATA
+ CATA
We get our products
  In shorter time; at lower rxn temperature; at lower pressure
  cheaper; economical; ecological

## Slide 3: Catalytic cycle
A + B → P
Ea >> Ea(cata); k = A∙e–Ea/RT
ΔG = ΔG(cata); ΔG = –RT∙lnK

## Slide 4: Kinetics
We know kinetics (#ChemKin)
Rxns of zero order, first order, and second order
But in catalysis also 0.39 order… (many steps, all contribute!)

## Slide 5: Kinetics
An important consideration: type of the reactor
  Batch
  Continuous (plug flow (fixed bed) reactor (PFR) or continuous stirred tank reactor (CSTR))
    Steady-state approximation (complicated math behind!)
    It is not possible to follow changes of concentrations in time

## Slide 6: Kinetics
Important terms
  Rate
  Arrhenius equation

## Slide 7: Kinetics
Important terms
  Reaction order
  For elementary reactions α, β = whole numbers (integers)
  For non-elementary reactions (i.e. catalytic reactions) α, β = non-integers

## Slide 8: Kinetics
Important terms
  Reaction order
    Can be negative!

## Slide 9: Kinetics
Important terms
  Reaction order
    Example: Determination of reaction order

## Slide 10: Kinetics
Back to Arrhenius equation
k – is the reaction rate constant
k – is not a constant in fact
  It depends on temperature and pressure
  Its units differ according to the reaction order

## Slide 11: Kinetics
Important terms
  Reaction pseudo-order
    Application of one (or more) of the reactants in a big excess so that its concentration in time t virtually equals concentration in time 0
    Simplification of reaction rate equation

## Slide 12: Kinetics

## Slide 13: Kinetics

## Slide 14: Kinetics
Ea (apparent) and A can be estimated by plotting ln k vs. 1/T = Arrhenius plot

## Slide 15: Kinetics
Summary

## Slide 16: Homework 1

## Slide 17: Homework 1

## Slide 18: Mechanisms of catalytic reactions
Langmuir (monomolecular)
  A(adsorbed) → P(adsorbed)
Langmuir-Hinshelwood (bimolecular)
  A(adsorbed) + B(adsorbed) → P(adsorbed)
Eley-Rideal (bimolecular)
  A(adsorbed) + B(gas phase) → P(adsorbed)
Mars-van Krevelen (special case)

## Slide 19: Mechanisms of catalytic reactions
Langmuir (monomolecular)
  A(adsorbed) → P(adsorbed)
Langmuir-Hinshelwood (bimolecular)
  A(adsorbed) + B(adsorbed) → P(adsorbed)
Eley-Rideal (bimolecular)
  A(adsorbed) + B(gas phase) → P(adsorbed)
Mars-van Krevelen (special case)

## Slide 20: Langmuir
Hypotheses identical as for Langmuir adsorption isotherm
  Monolayer
  One molecule per active site
  The enthalpy of adsorption independent on surface coverage Θ
    All sites identical
    No interactions between molecules of adsorbate
  Adsorption and desorption in equilibrium

## Slide 21: Langmuir
Reaction rate ≈ k∙[A]
First order reaction
Note:
k can be kA→P
Or
kA-adsorption

## Slide 22: Langmuir
Surface is fully covered with A
No change with increasing [A]
Reaction rate ≈ k
Zero order reaction
Note:
k can be kA→P
Or
kP-desorption

## Slide 23: Mechanisms of catalytic reactions
Langmuir (monomolecular)
  A(adsorbed) → P(adsorbed)
Langmuir-Hinshelwood (bimolecular)
  A(adsorbed) + B(adsorbed) → P(adsorbed)
Eley-Rideal (bimolecular)
  A(adsorbed) + B(gas phase) → P(adsorbed)
Mars-van Krevelen (special case)

## Slide 24: Langmuir-Hinshelwood
Competition between A and B adsorbates for adsorption sites

## Slide 25: Mechanisms of catalytic reactions
Langmuir (monomolecular)
  A(adsorbed) → P(adsorbed)
Langmuir-Hinshelwood (bimolecular)
  A(adsorbed) + B(adsorbed) → P(adsorbed)
Eley-Rideal (bimolecular)
  A(adsorbed) + B(gas phase) → P(adsorbed)
Mars-van Krevelen (special case)

## Slide 26: Eley-Rideal

## Slide 27: Mechanisms of catalytic reactions
Langmuir (monomolecular)
  A(adsorbed) → P(adsorbed)
Langmuir-Hinshelwood (bimolecular)
  A(adsorbed) + B(adsorbed) → P(adsorbed)
Eley-Rideal (bimolecular)
  A(adsorbed) + B(gas phase) → P(adsorbed)
Mars-van Krevelen (special case)

## Slide 28: Mars-van Krevelen
Example: oxidation of toluene over V2O5
  Oxygen comes from crystal lattice (confirmed by isotope studies)
    Creation of oxygen vacancies
    Regeneration of catalyst with O2 in the feed
O2
Note:
Catalyst should not change during catalysis!
Compare with Langmuir-Hinshelwood and Eley-Rideal

## Slide 29: Mars-van Krevelen
Possible only with metal oxides, sulphides, etc., where metal can achieve variable oxidation states and coordinations
Catalyst works as a „bank“
  It can borrow you oxygen if needed
  It can save oxygen for worse times…
Selectivity might be very high
  Specific oxidation species within the crystal lattice
Diffusion in solids needs to be considered
  Vacancies play an important role

## Slide 30: Mars-van Krevelen
Possible only with metal oxides, sulphides, etc., where metal can achieve variable oxidation states and coordinations:
  Oxidation of propylene to acrolein over MoO3-x
  Reduction of benzoic acid to benzaldehyde over MoO3-x
  Hydrodesulfurization of DBT do DB over NiMoS2-x
  Oxidation and reduction of gases in car exhausts over CeO2-Ce2O3

## Slide 32: Thermodynamics + steps of cat reaction
A + B → P
1
1: Adsorption of reactants on catalyst surface
2
3
1
3: Desorption of products from catalyst surface
2: Reaction on active site

## Slide 33: Steps of catalytic rxns
A + B → P
1
1: Diffusion medium→catalyst
2: Adsorption of reactants
(3: Diffusion on cat. surface)
4: Reaction on active site
(5: Diffusion on cat. surface)
6: Desorption of products
7: Diffusion catalyst→medium
4
6
2

## Slide 34: Steps of catalytic rxns
1a: Diffusion of the reactant in the fluid film surrounding the catalysts grain (External diffusion; macroporosity)
1b: Diffusion of the reactant in porous network until reaching surface (Internal diffusion; micro- and mesopores)
2: Adsorption of reactants
(3: Diffusion on cat. surface)
4: Reaction on active site
(5: Diffusion on cat. surface)
6: Desorption of products
7a: Diffusion of the product in the porous network until reaching the aperture of the pore (Internal diffusion)
7a: Diffusion of the product in the fluid film (External diffusion)

## Slide 35: Rate determining step
Total: Up to 9 steps; 6 of them diffusion!
All of them more or less contribute to the final reaction rate (kapparent and Eapparent)
Slowest step???

## Slide 36: Rate determining step
6 steps based on diffusion
  Fick laws
  Low dependance on temperature
  Ea = 4–8 kJ mol–1
3 steps based on chemistry
  High dependance on temperature
  Ea = 20–200 kJ mol–1
Slowest step of the catalytic reaction???
Depends on the temperature!!!
k = A∙e–Ea/RT

## Slide 37: Rate determining step
Low temperature
  Chemical steps are limiting
  Eapp = Ea of the reaction step

## Slide 38: Rate determining step
High temperature
  The chemical reaction is fast
  There is no time for internal diffusion to take place, only external surface employed in catalysis
  Diffusional steps are limiting
  Eapp = Ea of the diffusion in the fluid film (external diffusion)

## Slide 39: Rate determining step
Intermediate temperature
  Contribution of both chemistry and diffusion (diffusion in the pores, internal diffusion)
  Eapp = average of Ea of the reaction step and Ea of internal diffusion

## Slide 40: Diffusional limitation
kd = diffusion constant; ki = reaction rate constant per m2 of catalysts; S = specific surface area
kd = ki∙S; Surface is supplied with reactants; no diffusional limitation
kd << ki∙S; Internal surface of the catalyst is not supplied with reactants; Diffusional limitation

## Slide 41: Diffusional limitation
Gradient of reactant concentration in
  Fluid film of particle (External diffusion)
  Inside the pore (Internal diffusion)

## Slide 42: Diffusional limitation
We want to use as many active sites as possible (even deep in the internal pore system)
We want to avoid diffusional limitation
Effectivenes factor η (observed reaction rate / maximal theoretical reaction rate) depends on Thiele modulus
Thiele modulus φ describes the „quality“ of catalyst grain in terms of internal diffusion:
dp = diameter of grain; ki = reaction rate constant per m2 of catalysts; S = specific surface area; ρg = density of the catalyst including pores; De = diffusion coefficient of the reactant in the pores

## Slide 43: Diffusional limitation
Thiele modulus φ describes the „quality“ of catalyst grain in terms of internal diffusion:
The higher the Thiele modulus, the higher probability of diffusional limitations to occur
Internal diffusional limitations occur always to some extent

## Slide 44: Diffusional limitation
Thiele modulus φ describes the „quality“ of catalyst grain in terms of diffusion:
Let‘s decrease dp = small catalyst grains
Let‘s decrease ρg = higher pore volume
Let‘s increase De = bigger pores
Catalyst synthesis,
shaping, thermal
treatment…
…in order to avoid the internal diffusional limitations as much as possible…

## Slide 45: Diffusional limitation
Gradient of reactant concentration in
  Fluid film of particle (External diffusion)
    Viscosity of vector gas
    Linear velocity of vector gas
    Size of the grains
    Diffusion coeff of reactants
  Inside the pore (Internal diffusion)

## Slide 46: Diffusional limitations
Note: Up to now we have discussed only diffusion of reactants
Same applies for heat diffusion
I.e. diffusional limitations can lead to important issues!
  Effectivenes factor η > 1
  Hot spots
  Sintering of catalysts
  Shift/loss of selectivity
  Explosion
Industrial point of view

## Slide 47: Diffusional limitations
Internal diffusional limitations always present to some extent
  We can diminish them at the time of catalyst preparation (pore volume, pore diameter, size of catalysts grains)
External can be avoided at the time of catalytic reaction
  Linear velocity of vector gas,…
How to reveal external diffusional limitations?

## Slide 48: Diffusional limitations
How to reveal external diffusional limitations?
Constant temperature and constant contact time (other parameters can vary) lead to constant conversion, selectivity, and yield

## Slide 49: Diffusional limitations
How to reveal external diffusional limitations?
Contact time practically???
1 unit of catalyst mass
1 unit of catalyst volume
0.5 unit of catalyst mass
0.5 unit of catalyst volume
1 unit of linear gas velocity
1 unit of reactant feed
0.5 unit of linear gas velocity
0.5 unit of reactant feed
Conversion, yield, and selectivity are equal!
If not, then we encounter external diffusional limitations!

## Slide 50: Space velocity and contact time
Contact time = 1/space velocity
Space velocity [h–1]
  Based on catalyst mass (WHSV, weight hourly space velocity)
    weight of reactant per weight of catalyst per hour
  Based on catalyst volume (GHSV or LHSV – gas/liquid…)
    Volume of feed gas@STP (reactant + gas vector) per volume of catalyst bed per hour
Be careful, contact time can be based on WHSV, GHSV, or LHSV!

## Slide 51: Space velocity and contact time
Calculations with volumes always much less convenient than weight…
So…Why is GHSV/LHSV important in heterogeneous catalysis??
1 unit of catalyst mass
1 unit of catalyst volume
1 unit of catalyst mass
1 unit of catalyst volume
1 unit of linear gas velocity
Feed of reactant constant
0.5 unit of linear gas velocity
Feed of reactant constant
WHSV is constant. GHSV is different.
Conversion, yield, and selectivity are different!

## Slide 52: Space velocity and contact time
1 unit of catalyst mass
1 unit of catalyst volume
1 unit of linear gas velocity [m3 h–1]
1 unit of reactant feed
Mass flow controller
Soap bubble flow meter

## Slide 53: Space velocity and contact time
1 unit of catalyst mass
1 unit of catalyst volume
1 unit of linear gas velocity
1 unit of reactant feed [g or cm3 h–1]
→ gas
(= mass flow control, soap…)
→ liquid
Automatic syringe pump
Vapor saturator (= bubbler)

## Slide 54: Space velocity and contact time
1 unit of catalyst mass [g]
1 unit of catalyst volume [cm3]
1 unit of linear gas velocity
1 unit of reactant feed
→ dilute with inert material to a constant volume
Remember,
GHSV important for catalyst comparison

## Slide 55: Homework 2
Selectivity = 90 % in all cases; WHSV = 15.5 h–1
2
-2 MeOH
TiO2/SiO2
Temperature [°C] | Conversion sample 1 (4.2 wt% Ti) [%] | Conversion sample 2 (0.9 wt% Ti) [%]
220 | 39 | 8.6
230 | 48 | 9.6
240 | 59 | 13
250 | 82 | 17
260 | 93 | 21
Gas phase transesterification
Continuous flow fixed bed reactor
Create Arrhenius plots for both catalysts (plot ln k [molLD gcat–1 h–1] vs. 1000/T [K–1]
Estimate apparent Ea and A from Arrhenius equation
What makes the difference between these two catalysts?
ACS Catal. 2018, 8, 9, 8130–8139