## Slide 1: Heterogeneous catalysis
Lecture 3
Catalysts preparation

## Slide 2: Types of catalysts
Bulk catalysts
Supported catalysts
Malaxed-agglomerated catalysts

## Slide 3: Types of catalysts
Bulk catalysts
Supported catalysts
Malaxed-agglomerated catalysts
  Intermediate category
  Catalysts obtained by mixing active species with support (powders+precursors)
  Ill defined catalysts – broad application in industry

## Slide 5: Types of catalysts
Bulk catalysts
Supported catalysts
Malaxed-agglomerated catalysts

## Slide 6: Preparation of bulk catalysts
The whole body of the catalyst is made of one active substance
= It must be cheap, thermally, mechanically, and chemically stable, porous,…!
  Silica-alumina (cracking)
  Raney nickel, Co molybdate (hydrogenation)
  Catalyst supports: silica, alumina, silica-alumina, zeolites, TiO2, MgO, carbon

## Slide 7: Preparation of bulk catalysts
Ceramic route (heat and beat)
  e.g. Molybdates Bi2O3 + MoO3 → Bi2MoO6
  Used as selective oxidation catalysts (propylene to acrolein)
  Homogeneity, time, temperature
(Co-)Precipitation
  E.g. NH4VO3 + Al(NO3)3 → V-Al oxynitride (used in propene ammoxidation to acrylonitrile)
  change of pH leads to precipitation
Sol-gel method
Combustion synthesis
Solvothermal method
  e.g. zeolites

## Slide 8: Preparation of bulk catalysts
Ceramic route, (co-)precipitation, sol-gel method, combustion synthesis, and solvothermal method: #InorgMatChem
Heat and beat quickly and effectively?
Sol-gel continuously???
Ball milling!
Aerosol assisted
sol-gel process!

## Slide 9: Preparation of bulk catalysts

## Slide 10: Preparation of bulk catalysts

## Slide 11: Preparation of bulk catalysts
◊ γ-AlOOH
● α-Al2O3
Δ α-AlOOH

## Slide 12: Preparation of bulk catalysts

## Slide 13: Preparation of bulk catalysts

## Slide 14: Types of catalysts
Bulk catalysts
Supported catalysts
Malaxed-agglomerated catalysts

## Slide 15: Preparation of supported catalysts
Properties of catalyst supports
  Cheap
  Porous
  Thermally, mechanically, and chemically stable
  …
Role of catalyst supports (non-innocent)
  Porosity/hydrophobicity vs. Activity/selectivity
  O, H, N,…bank (MvK mechanism)
  Electron donor/acceptor (Haber-Bosch)
  …

## Slide 16: Preparation of supported catalysts
Three types of interaction between support and active phase
  Weak
  Electrostatic
  Covalent

## Slide 17: Preparation of supported catalysts
Weak interaction = Impregnation methods
  Wet impregnation
    Suspension of support (e.g. SiO2 in water)
    Solution of metal salt (e.g. Cu(NO3)2 in water)
    Mixed together (suspension)
    Cu2+ cations diffuse into the pores of SiO2 support (=we need to wait for enough long time, Fick laws)
    Drying, calcination (= formation of Cu2O NPs on SiO2), (reduction of Cu2O to Cu NPs)
    Disadvantages: Time, homogeneity.

## Slide 18: Preparation of supported catalysts
Weak interaction = Impregnation methods
  Dry impregnation (Incipient wetness impregnation)
    Dry support, pores full of gas (e.g. SiO2 in ambient air)
    Solution of metal salt, V = pore volume (e.g. Cu(NO3)2 in water)
    Mixed together (paste)
    Capillary elevation (fast) brings Cu2+ solution directly into the pores (concentration gradients might occur – pore size!)
    Drying, calcination (= formation of Cu2O NPs on SiO2), (reduction of Cu2O to Cu NPs)
    Solubility limits!

## Slide 19: Preparation of supported catalysts
Weak interaction = Impregnation methods
  Dry impregnation (Incipient wetness impregnation)
    Big issue: Gas trapped inside the pores
    Pore collapse
    Mechanical degradation
    Attrition
    …

## Slide 20: Preparation of supported catalysts
Weak interaction = Impregnation methods
  Dry impregnation (Incipient wetness impregnation)
    Big issue: Gas trapped inside the pores
    Possible solutions:
    No gas (impregnation under vacuum)
    Lower surface tension (addition of a surfactant)
    Wait until gas dissappears and impregnation is completed (either gas dissolves in solution or bubbles move out from the pores)

## Slide 21: Preparation of supported catalysts
Weak interaction = Impregnation methods
  Dry impregnation (Incipient wetness impregnation)
    Big issue: Gas trapped inside the pores

## Slide 22: Preparation of supported catalysts
Three types of interaction between support and active phase
  Weak
  Electrostatic
  Covalent

## Slide 23: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Classic ion exchangers: clays, layered hydroxides, zeolites
  Oxides with the help of pH

## Slide 24: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Zeolites, how does it work?
  Cation compensating the negative charge?
  Na+ from the synthetic step

## Slide 25: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Zeolites, how does it work?
  Na+ → H+ directly?
  Na+ → ??? → H+

## Slide 26: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Zeolites, how does it work?
  Na+ → NH4+ → H+
  Zeolite NaY
  Up to 73 % of Na+ can be exchanged at R.T.
  4 consecutive steps or continuous ion exch.
  ΔT

## Slide 27: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Enhancement…trap for leaving ion (shifting equilibrium)!
  e.g. Exchange of Ni2+ for H+ in zeolite mordenite
  Ni(NO3)2 vs. Ni(OAc)2

## Slide 28: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Trap
    OAc- + H+ → AcOH (rarely dissociated)
    OH- + H+ → H2O (rarely dissociated)
    SCN- + Ag+ → AgSCN (rarely dissociated)
Salt - trap
Support

## Slide 29: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Classic ion exchangers: clays, layered hydroxides, zeolites
  Oxides with the help of pH

## Slide 30: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH

## Slide 31: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Isoelectric point

## Slide 32: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Exchange capacity: the farther you are from isoelectric point, the higher the exchange capacity.

## Slide 33: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Stability of support at different pH!
    Precursor stability at different pH!
Hydrolysis, condensation,
precipitation…!

## Slide 34: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Competitive ion exchange
    Example: very high affinity between Al2O3 and Pt
    Result: heterogeneous distribution of Pt (only outer surface)

## Slide 35: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Competitive ion exchange
    NH4OH dissociates readily, NH4+ competes with Pt for sites (= inverse to trap)
    Result: homogeneous distribution of Pt through the support
2–

## Slide 36: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Competitive ion exchange
    [NH4+]

## Slide 37: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Competitive ion exchange

## Slide 38: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Competitive ion exchange

## Slide 39: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Competitive ion exchange: Note
    We say homogeneous Pt distribution…
    But how homogeneous???
    Latest research from de Jong group (University Utrecht, HR-TEM, perfect control of Pt deposition on atomic scale) shows that uniform Pt homogeneity is not ideal for hexane isomerization!

## Slide 40: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Detailed knowledge of isoelectric point, precursor behavior, control over pH:

## Slide 41: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH
    Detailed knowledge of isoelectric point, precursor behavior, control over pH:

## Slide 42: Preparation of supported catalysts
Electrostatic interaction = Ion exchange
  Oxides with the help of pH

## Slide 43: Preparation of supported catalysts
Three types of interaction between support and active phase
  Weak
  Electrostatic
  Covalent

## Slide 44: Preparation of supported catalysts
Covalent bonds = grafting
  Formation of metal oxide on top of catalyst support
  Is calcination necessary? More in lecture on single site catalysts…

## Slide 45: Preparation of supported catalysts
Covalent bonds = grafting
  Formation of metal NPs on top of catalyst support

## Slide 46: Preparation of supported catalysts
Covalent bonds = grafting
  NPs by impregnation vs. grafting
calcination
Covalent bonds
Uniform NPs

## Slide 47: Preparation of supported catalysts
Covalent bonds = grafting
  Formation of metal NPs on top of graphene oxide
Content of COOH groups
increased by oxidation
(HNO3, H2O2,O3,…)

## Slide 48: Preparation of supported catalysts
Covalent bonds = grafting
  Formation of metal NPs on top of graphene oxide
  Last step: Pd reduction

## Slide 49: Preparation of supported catalysts
Covalent bonds = Deposition/precipitation
  Starts as a dry impregnation
  Metal salt is then selectively precipitated at the catalyst surface
  Precipitation mainly by pH change – hydrolysis/condensation