## Slide 1: Heterogeneous catalysis
Lecture 6
Catalysts characterization - continuation

## Slide 2: Catalyst characterization
Outline
  Special MAS NMR techniques
  Hydrophilicity vs. Hydrophobicity meas
    Water sorption
    Dynamic water sorption
    Inverse gas chromatography
    Microcallorimetry
    Quartz crystal microbalance
  In situ and operando techniques

## Slide 3: Special MAS NMR techniques
MQMAS
DNP

## Slide 4: Hydrophilicity vs. Hydrophobicity
Why?
  Remember: Adsorption/desorption step in cata as important as cata rxn itself (@Lecture 1)
  Moreover: strong efforts nowadays put forward bio-sources instead of fossil fuels
  Compare
    Oil – long hydrocarbon chains (hydrophobic)
    Wood – cellulose, lignin = sugar based materials = a lot of oxygen, OH groups (hydrophilic)

## Slide 5: Hydrophilicity vs. Hydrophobicity
Possibilities:
  Water sorption
  Dynamic vapor sorption/Quartz crystal microbalance
  Inverse gas chromatography
  Microcallorimetry

## Slide 6: Hydrophilicity vs. Hydrophobicity
Problems:
  What is a measure of hydrophobicity?
    A material can have high/low affinity to both water and organic molecules (i.e. if a sample is hydrophilic, it does not necessarily mean it is hydrophobic!)
      % of pore volume filled with water at certain p/p0
      Hydrophobic index (water/toluene competitive sorption)
      Heat of adsorption, heat of immersion
      …
  Chemisorption: Do chemisorbed molecules account for hydrophobicity/philicity?

## Slide 7: Hydrophilicity vs. Hydrophobicity
Water sorption
  Similar to N2 physisorption
  Known volume and pressure in the cell, known mass of the sample

## Slide 8: Hydrophilicity vs. Hydrophobicity
Water sorption
Very strong interaction water-adsorbent
Very weak interaction water-adsorbent
Water clustering = water-water interaction (liquefaction, condensation) stronger than water-adsorbent

## Slide 9: Hydrophilicity vs. Hydrophobicity
Water sorption
  Plotting ln p against 1/T at constant adsorption uptake gives a straight line with a slope equal to Hiso/R
  Hiso = isosteric heat of adsorption
  Isotherms at multiple temperatures needed!

## Slide 10: Hydrophilicity vs. Hydrophobicity
Water sorption
  Hiso = isosteric heat of adsorption
Hydrophobic material = very low Hiso = negligible interaction water-adsorbent
Hydrophilic material = very high Hiso = strong interaction water-adsorbent
Hiso more or less constant = water-water interaction (condensation)

## Slide 11: Hydrophilicity vs. Hydrophobicity
Dynamic vapor sorption/Quartz crystal microbalance
  You deposit your material on an accurate microbalance
  You expose it to vapors of different gases/liquids (water, alcohols, hydrocarbons,…)
  You follow the uptake by changes of mass
  If we can control/follow pressure, then isotherms can be obtained similar to a classic physisorption

## Slide 12: Hydrophilicity vs. Hydrophobicity
Inverse gas chromatography
  You pack column (≈ 50 cm) with the material you want to test (≈ 0.5 g)
  You inject series of gases/liquids (e.g. methane, ethane,…hexane, heptane; methanol, ethanol,…; benzene, toluene, xylene…)
  You follow retention time (you directly see „affinity“ of your material to selected liquids)
  Models (math) can give surface energy,…

## Slide 13: Hydrophilicity vs. Hydrophobicity
Immersion microcalorimetry
  Evacuated sample sealed in a bulb with brittle end
  Bulb immersed in a testing liquid, sealed
  Bulb broken (rod pushed down)
  Liquid gets into the bulb, adsorbs, heat of immersion released and measured

## Slide 14: Hydrophilicity vs. Hydrophobicity
Immersion microcalorimetry
  Ti-MCM-41, pure inorganic vs. increasing degree of surface silylation (increasing carbon content)
J. Silvestre-Alberó et al. / Applied Catalysis A: General 507 (2015) 14–25

## Slide 15: In situ and operando techniques
In situ = online analysis of a working catalyst
Operando = online analysis of a working catalyst at relevant conditions (p, T, WHSV)

## Slide 16: In situ and operando techniques
We already know these techniques, let‘s look at the examples!
  Low energy electron diffraction (LEED, gives similar results to x-ray diffraction = analysis of crystal structures)
  X-ray absorption near edge structure (XANES)
  Diffusive reflectance infrared Fourier transform spectroscopy (DRIFTS)

## Slide 17: In situ and operando techniques
Example: LEED – low energy electron diffraction
Ethylbenzene dehydrogenation to styrene
  600 °C, 1 atm, 10-fold excess water vapor
  Over Fe2O3 epitaxially grown on Pt(111)
Flow reactor located in a high pressure cell
  Heated by lasers
  GC-MS analysis of catalytic products
  LEED analysis enabled by gate valve (high pressure/ultra high vacuum) and sapphire window

## Slide 18: In situ and operando techniques
Example: LEED – low energy electron diffraction

## Slide 19
Before catalytic reaction
After catalytic reaction
Initial period, no catalytic activity
Working catalyst

## Slide 20: In situ and operando techniques
Example: LEED – low energy electron diffraction
Active catalyst
Non-crystalline Fe2O3
Metastable (Reduction!)
Carbon deposition (Styrene!)
Loss of catalytic activity
0.5 eq O2 addition

## Slide 21: In situ and operando techniques
Example: XANES – x-ray absorption near edge structure
Methanol oxidation to formaldehyde over Cu
  25–450 °C, 1 mbar
  Cu in the form of polycrystalline foil
  2 CH3OH + O2 → 2 CH2O + 2 H2O

## Slide 22: In situ and operando techniques
Example: XANES – x-ray absorption near edge structure
  2 CH3OH + O2 → 2 CH2O + 2 H2O

## Slide 23: In situ and operando techniques
Example: XANES – x-ray absorption near edge structure
2 oxide and 1 suboxide species

## Slide 24: In situ and operando techniques
Example: XANES – x-ray absorption near edge structure
Positive correlation between catalytic activity and Cu suboxide species
Explanation/idea/description of active species: Subsurface oxygen cover by a strained layer of copper atoms
Results confirmed by near ambient pressure XPS (NAP XPS)

## Slide 25: In situ and operando techniques
Example: DRIFTS – diffuse reflectance infrared Fourier transform spectroscopy
Coupling of ethanol and acetaldehyde to 1,3- butadiene over Ta doped zeolite
  300 °C, 1 atm
  Well dispersed (virtually isolated) Ta sites
  2 C2H5OH + CH3CHO → C4H6 + 2 H2O

## Slide 26: In situ and operando techniques
Example: DRIFTS – diffuse reflectance infrared Fourier transform spectroscopy

## Slide 28: In situ and operando techniques
Example: DRIFTS

## Slide 29: In situ and operando techniques
Example: DRIFTS – diffuse reflectance infrared Fourier transform spectroscopy