## Slide 1: Heterogeneous catalysis
Lecture 4
Catalyst synthesis – continuation
Shaping
Single site catalysts

## Slide 2: Shaping
Why is shaping important?
  Accessibility (micro+meso+macro porosity)
  Mechanical resistance (application of binders)
  Reducing pressure drop (p1 > p2)
  Hydrothermal stability, coking, poisoning,…
p2
p1
→ Industrial point of view

## Slide 3: Shaping
Industrial example: Fluid catalytic cracking

## Slide 4: Shaping
Fluid catalytic cracking
„agglomerated catalyst“

## Slide 5: Shaping
Industrial example: Fluid catalytic cracking
micrograin
Elementary particles

## Slide 6: Shaping
Macroscopic shaping
  Extrusion
  Pelletization
  Molding/casting
grain

## Slide 7: Shaping
Shaping as a „mechanochemical synthesis“?

## Slide 8: Single site catalysts
What is it?
Active site in cytochrome P450
Enzymatic catalysis
Grubbs catalyst
Homogeneous catalysis

## Slide 9: Single site catalysts
What is it?

## Slide 10: Single site catalysts
What is it?

## Slide 11: Single site catalysts
Any continuous material (metal, oxide), where catalysis relies mainly on structure deffects
Instead
  One (or more) atoms
  Spatially isolated
  Same energy of interaction with reactant
  Structurally well characterized (similar to homo)

## Slide 12: Single site catalysts
What is it?
  Individual isolated ion/atom/molecular complex/cluster
    Grafted on porous support
    Created within the material by building block approach
  „Ship in bottle“ structures– e.g. molecular complex/enzyme trapped within a zeolitic cage
  Crystalline, open-structure, microporous solids (e.g. zeolites) with active sites uniformly distributed throughout the bulk

## Slide 13: Single site catalysts
Why?

## Slide 14: Single site catalysts
Why?
  Number of active sites
  Turn-over frequency, TOF
  Characterization of active site
  Quantum-chemical calculations
  ↓
  Understanding mechanism
  Understanding kinetics
  ↓
  Bridging gap between homo-and heterogeneous cata

## Slide 15: Single site catalysts
Bridging gap between homogeneous and heterogeneous catalysis – example:
  Phillips catalyst = „CrO3“ dispersed on silica
  Ethylene polymerization (50 % of global production of linear HDPE)
  No co-catalyst (compare with Ziegler-Natta + MAO)
  What is the actual active site???

## Slide 16: Single site catalysts
CrO3 dispersed on silica
Ethylene exposure induces „mild reduction“
Only 10 % of Cr sites are active
CrII or CrIII??? Big discussion…

## Slide 17: Single site catalysts
CrII
CrIII

## Slide 18: Single site catalysts
CrIII is active!

## Slide 19: Single site catalysts
What is it?
  Individual isolated ion/atom/molecular complex/cluster
    Grafted on porous support
    Created within the material by building block approach
  „Ship in bottle“ structures– e.g. molecular complex/enzyme trapped within a zeolitic cage
  Crystalline, open-structure, microporous solids (e.g. zeolites) with active sites uniformly distributed throughout the bulk

## Slide 20: Single site catalyts
Grafting on silica
  Detailed knowledge of surface (number of OH groups per nm2)
  Rigorous water- and oxygen-free environment

## Slide 21: Single site catalysts

## Slide 22: Single site catalysts
Metal precursors (almost all d + f elements)
  Organometallic compounds
  Metal amides and silylamides
  Metal alkoxides and siloxides
  Metal halogenides

## Slide 23: Single site catalysts

## Slide 24: Single site catalysts
In many cases silica needed all around the active site (no unreacted chlorines etc.)
+ SiO2
2. ΔT
− butene
1.
− butanol

## Slide 25: Single site catalysts
Grafting on silica – other types of bonding

## Slide 26: Single site catalysts
Grafting on silica – other types of bonding

## Slide 27: Single site catalysts
Grafting on carbon – π-π stacking

## Slide 28: Single site catalysts
Grafting on carbon – π-π stacking
  Boomerang effect

## Slide 29: Single site catalysts
What is it?
  Individual isolated ion/atom/molecular complex/cluster
    Grafted on porous support
    Created within the material by building block approach
  „Ship in bottle“ structures– e.g. molecular complex/enzyme trapped within a zeolitic cage
  Crystalline, open-structure, microporous solids (e.g. zeolites) with active sites uniformly distributed throughout the bulk

## Slide 30: Single site catalysts
+ n MClx
Si8O20(SnMe3)8
=
SnMe3
MClx = PCl3, SiCl4, BBr3, AlCl3, GaCl3, TiCl4, ZrCl4, VCl4, VOCl3, SnCl4, WCl6, MoO2Cl2
-ClSnMe3
M
O
O
O
O
M
M
M
M
1. N.N. Ghosh, J.C. Clark, G.T. Eldridge, C.E. Barnes, Chem. Comm., (2004) 856-857.
2. M.-Y. Lee, J. Jiao, R. Mayes, E. Hagaman, C.E. Barnes, Catalysis Today, 160 (2011) 153-164.

## Slide 31: Single site catalysts
Si8O12(OSnMe3)8
O
Al
O
O
Si
S
i
C
l
4
Me3SnCl
RO
Al
Cl
Cl
Cl
R
Si
O
Si
Me3SnCl
Al
O
O
O
O
R
R
limiting
amount
R
R

## Slide 32: Single site catalysts
Targeting connectivity
Al
O
O
O
L
3C-Al←L
L = py (1), THF (2)
Al
O
O
O
O
X+
[X][4C-Al]
X = NBu4+ (3)

## Slide 33: Single site catalysts
Targeting geometry
  Tetrahedral
  Square planar
Ti
O
O
O
O
4C-Ti

## Slide 34: Single site catalysts
What is it?
  Individual isolated ion/atom/molecular complex/cluster
    Grafted on porous support
    Created within the material by building block approach
  „Ship in bottle“ structures– e.g. molecular complex/enzyme trapped within a zeolitic cage
  Crystalline, open-structure, microporous solids (e.g. zeolites) with active sites uniformly distributed throughout the bulk
CHARACTERIZATION?

## Slide 35: Single site catalysts
What is it?
  Individual isolated ion/atom/molecular complex/cluster
    Grafted on porous support
    Created within the material by building block approach
  „Ship in bottle“ structures– e.g. molecular complex/enzyme trapped within a zeolitic cage
  Crystalline, open-structure, microporous solids (e.g. zeolites) with active sites uniformly distributed throughout the bulk

## Slide 36: Single site catalysts
Cobalt phthalocyanine within zeolite Y

## Slide 37: Single site catalysts
Single site very well preserved (no dimerization,…)
Diffusion of molecules small enough in the micropore system of zeolite – both reactants and products – enhancing specificity and selectivity

## Slide 38: Single site catalysts
Synthesis?
  Cation exchange (2Na+ for Co2+)
  Complexation with ligands within the zeolite pores
„Co2+-exchanged zeolite-Y was heated with excess amount of 1,2-dicyanobenzene (DCB) under vacuum. Excessive DCB was then extracted (Soxhlet).
The dicyanobenzene molecule is small enough (∼6.5 Å) to diffuse through the 7.4 Å windows of the supercage of the zeolite and condense around the metal ion to form cobalt phthalocyanine.“

## Slide 39: Single site catalysts
Enzyme agglomerates inside a hollow silica sphere
Chem. Sci., 2020,11, 954-961

## Slide 40: Single site catalysts
What is it?
  Individual isolated ion/atom/molecular complex/cluster
    Grafted on porous support
    Created within the material by building block approach
  „Ship in bottle“ structures– e.g. molecular complex/enzyme trapped within a zeolitic cage
  Crystalline, open-structure, microporous solids (e.g. zeolites) with active sites uniformly distributed throughout the bulk

## Slide 41: Single site catalysts
Zeolites
  ≡Si−O(H)−Al≡
MAlPOs
  ≡MII−O(H)−P≡
  M = Mg, Co, Zn, Mn…

## Slide 42: Single site catalysts
Zeolites and MAlPOs
  Microporous
  Crystalline
  Ideal to study by many analytical techniques

## Slide 43: Single site catalysts
Zeolites and MAlPOs
  Isolated sites???
    Si/Al ratio ≥ 200; perfect crystallinity
  Equivalent sites???
  Amorphous grains/surface species

## Slide 44: Single site catalysts
Zeolites and MAlPOs
  Isolated sites???
  Equivalent sites???
    Different positions in cage
  Amorphous grains/surface species

## Slide 45: Single site catalysts
Zeolites and MAlPOs
  Isolated sites???
  Equivalent sites???
  Amorphous grains/surface species
    e.g. extraframework aluminum species
      From not fully embedded (connectivity = 3) surface Al atoms to amorphous alumina (nano)particles
      Tetra, penta, hexacoordinated
      Easy to overlook (99 % of the material is crystalline), but important to notice
      Their role in catalysis???

## Slide 46: Single site catalysts
Similar but different (Markus Antoinetti et al.)
Doped graphene sheets
Isolated sites located by HR-TEM

## Slide 47: Single site catalysts
Doped graphene sheets
  Single metal atoms within carbon layer
    Single atom = „complex like“
    Conductive carbon layer, electrons shared = „metal like“
    Unique
    Single-site Au highly active in Haber-Bosch ammonia synthesis, mild conditions

## Slide 48: Single site catalysts
Doped graphene sheets
  Single Au atoms within N-doped graphene

## Slide 49: References