## Slide 1: Heterogeneous catalysis
Lecture 5
Catalysts characterization

## Slide 2: Catalyst characterization
Outline
  DRUV
  XPS
  XANES & EXAFS
  Chemisorption
  ToF-SIMS

## Slide 3: Diffuse reflectance UV-Vis spectroscopy (DRUV)
Is there any link between reflectance and absorbance?
Yes, there is!
Kubelka-Munk model allows to obtain quantitatively the absorption spectrum of a solid from diffuse reflectance measurement (theory behind in textbooks)
I
J

## Slide 4: Diffuse reflectance UV-Vis spectroscopy (DRUV)
LMCT = ligand-to-metal charge transfer
MLCT = metal-to-ligand charge transfer
MMCT = metal-to-metal charge transfer

## Slide 5: Diffuse reflectance UV-Vis spectroscopy (DRUV)

## Slide 6
Photoelectron spectroscopy:
  UV: valence shell ionizations
  X-ray: core electron ionizations (XPS, XANES, EXAFS):
valence
levels
core
levels
virtual
levels
ionization
continuum
Ephoton = hν =
BE + kinetic energy (KE)
0
BE
KE
Photoelectron Spectroscopy analyzes the energies of the ionized electrons (XPS).
X-ray Absorption Spectroscopy analyzes the absorption curve of the X-ray spectrum associated with ionization of a core electron (XANES and EXAFS)
Ionization Spectroscopies

## Slide 7: X-ray photoelectron spectroscopy (XPS)
We measure the number and the energy of photoelectrons emitted from the surface layer
Ephoton = hν =
BE + kinetic energy (KE)
Number of photoelectrons gives access to quantity
Energy of photoelectrons gives access to quality
Depth? 5–20 nm.

## Slide 8: X-ray photoelectron spectroscopy (XPS)
Auger

## Slide 9: X-ray photoelectron spectroscopy (XPS)
Surface vs. bulk composition
Surface
Bulk
Calcination
K. Bouchmella et al. /Journal of Catalysis 301 (2013) 233–241

## Slide 10: X-ray photoelectron spectroscopy (XPS)
Oxidation state
Binding energy [eV]
0
1000
C0
CI
CII
CIII
CIV
?
Who will hold its electrons more powerfully? C0 or CIV?

## Slide 11: X-ray photoelectron spectroscopy (XPS)
Oxidation state
Binding energy [eV]
0
1000
C0
CI
CII
CIII
CIV
Why do we talk about carbon?
Surface of each sample contains some carbon impurities = Adventitious carbon = calibration of BE

## Slide 12: X-ray photoelectron spectroscopy (XPS)
Oxidation state

## Slide 13: X-ray photoelectron spectroscopy (XPS)
Similar consideration:
SiO4 vs. CSiO3
Ta(OSi)x(OTa)6-x vs. Ta(OTa)6
Electronegativity (O) =
Electronegativity (C) =
Electronegativity (Si) =
Electronegativity (Ta) =

## Slide 14: X-ray photoelectron spectroscopy (XPS)
Spin-orbital interaction and other electron interactions lead to additional features in XP spectra characteristic for
  Oxidation states
  Groups
  …
Characteristic for Mn2+

## Slide 15: X-ray photoelectron spectroscopy (XPS)
Spin-orbital interaction and other electron interactions lead to additional features in XP spectra characteristic for
  Oxidation states
  Groups
  …
Characteristic for
aromatic carbon

## Slide 16
Photoelectron spectroscopy:
  UV: valence shell ionizations
  X-ray: core electron ionizations (XPS, XANES, EXAFS):
valence
levels
core
levels
virtual
levels
ionization
continuum
Ephoton = hν =
BE + kinetic energy (KE)
0
BE
KE
Photoelectron Spectroscopy analyzes the energies of the ionized electrons (XPS).
X-ray Absorption Spectroscopy analyzes the absorption curve of the X-ray spectrum associated with ionization of a core electron (XANES and EXAFS)
Ionization Spectroscopies

## Slide 17: XANES and EXAFS
In XANES and EXAFS we measure number and energy of transmitted photons, which caused ionization of a core electron
(i.e. absorbance vs. energy)
X-ray storage ring
Iref
Io
It
Ifluor
Sample
Monochromator
Metal
Reference
Foil
Synchrotron
    Energy needed is so much greater
    than that available from a
    typical X-ray tube found in most labs

## Slide 18: XANES and EXAFS
XAS: X-ray absorption spectroscopy; alternatively XAFS: X-ray absorption fine structure
  XANES: X-ray absorption near edge structure (pre-edge); alternatively NEXAFS (near edge x-ray absorption fine structure)
  EXAFS: Extended x-ray absorption fine structure (= behind edge)
What is an edge?

## Slide 19: XANES and EXAFS
valence
levels
core
levels
virtual
levels
Edge = 0
BE
KE
EXAFS
XANES

## Slide 20: XANES and EXAFS
XANES
EXAFS

## Slide 21: XANES
Qualitative information on coordination environment (dipole selection rules apply)
  Is there a pre-edge feature?
    Yes – no inversion center
    No – there is an inversion center
Quantitative info also possible
Figure from Farges, et. al. Physical Review B: Condens. Matter 1997, 56(4), 1809-1819.

## Slide 22: XANES
Coordination environment

## Slide 23: XANES
Position of the edge…binding energy…oxidation state

## Slide 24: EXAFS
Eo
Relative absorbance [a.u.]
XANES
EXAFS
What type of information is hidden there???
Energy
Absorbance

## Slide 25: EXAFS
The scattering phenomena
Scattering from Ti
Back-scattering
from “neighbors”

## Slide 26: EXAFS
k3 c(k) (Å-3)
0
5
10
-5
-10
0
5
10
15
k (Å-1)
c(k)
Eo
Arbitrary Units
EXAFS
Step 1: The data
Step 2: Extract c(k)
Step 3: The FT
Step 4:
Develop structural model that fits that data
d(M-X), CN(X),
AtNum(X)
Fourier Transform
Math

## Slide 27: EXAFS
— Ti(Si8O20)4
— FEFF 8 fit
5
0
10
|c(R)| (Ǻ-4)
0
1
2
3
4
5
6
Ti
O
O
O
O
0
1
2
3
4
5
6
R (Ǻ)
5
0
10
15
|c(R)| (Ǻ-4)
Ti
O
O
Cl
Cl
Ti–O
Ti∙ ∙ ∙ Si
Ti–O
Ti∙ ∙ ∙ Si
Ti–Cl
Structure elucidation of an amorphous material!
If more Ti sites, than average; analysis more difficult!

## Slide 28: Chemisorption
Interactions of A,B, and P with catalyst not too weak, not too strong (= physi/chemisorption on catalyst surface)
Sabatier‘s principle;
Volcano plot@Lecture 1

## Slide 29: Chemisorption
Different sites = different probes
  Acid sites
    NH3, alkylamines, pyridine, 2,6-dimethylpyridine, CO
  Basic sites
    CO2
  Redox
    H2, O2, N2O
  Reactants can be used as probes
    e.g. ethanol dehydration = I can study chemisorption of ethanol

## Slide 30: Chemisorption
Different ways how to do it
  Volumetric
  Thermally programmed desorption/oxidation/reduction
  Pulse titration
  Chemisorption of IR (NMR) active molecules and their analysis by IR (NMR)

## Slide 31: Chemisorption
Volumetric
  Similar to N2 physisorption (glass tube of known volume, addition of known volume of gas, pressure measurement)
  NH3 adsorption isotherms measured twice, sample evacuated between the two measurements (physisorption vs. chemisorption)
  High temperatures in contrary to N2 physisorption (e.g. 50 °C)

## Slide 32: Chemisorption
Volumetric
1st isotherm
2nd isotherm
Difference 1st – 2nd
=
chemisorbed NH3
Uptake
=
physisorption + chemisorption
Uptake
=
physisorption only
(chemisorbed NH3 already there)
evacuation
Temperature?

## Slide 33: Chemisorption
Thermally programmed desorption/oxidation/reduction
Detector
(MS, TCD)
Furnace

## Slide 34: Chemisorption
Thermally programmed desorption/oxidation/reduction
Time
Temperature [°C]
NH3
Ar
Ar
150
500
700
Dehydration
Pretreatment
Desorption
Analysis
Chemisorption
Temperature?

## Slide 35: Chemisorption
Thermally programmed …
NH3 TPD

## Slide 36: Chemisorption
Pulse titration

## Slide 37: Chemisorption
Pulse titration

## Slide 38: Chemisorption
Pulse titration
  Correct choice of gas (H2, CO, O2, N2O)
  Correct choice of temperature
    = Monolayer
    = Dispersion, particle size, „active metal surface area“
Number of surface
atoms
Total number of
atoms

## Slide 39: Chemisorption
Pulse titration
  Very good correlation can be observed between active surface area by H2 chemisorption and activity in hydrogenation of … for classical hydrogenation catalyts (Pt, Pd)
  H2 chemisorption is dissociative!
  H–H bond breaks at the time of chemisorption, this is the key to high reactivity (adsorbed molecular hydrogen)
  This is Langmuir‘s chemistry
Pt Pt Pt
H H H

## Slide 40: Chemisorption
X2 dissociative chemisorption (detour)
Pt Pt Pt
H H H
2A, ad
A2, ad
A2
Ediss, noncatalyzed
Ea
O2 adsorption on Pt(111) surface @165 K
O–O in O2 = 1.2Å, here much longer
„Hot“ O atoms
Lifetime 10–13 s

## Slide 41: Chemisorption
Pulse titration
  Very good correlation can be observed between active surface area by H2 chemisorption and activity in hydrogenation of … for classical hydrogenation catalyts (Pt, Pd)
  BUT
Example: methanol synthesis over Cu NPs
  CO2 + 2 H2 → CH3OH
Pt Pt Pt
H H H
Science 18 May 2012: Vol. 336, Issue 6083, pp. 893-897

## Slide 42: Chemisorption
Example: methanol synthesis over Cu NPs

## Slide 43: Chemisorption
Example: methanol synthesis over Cu NPs

## Slide 44: Chemisorption
Example: methanol synthesis over Cu NPs

## Slide 45: Chemisorption
Pulse titration
  Homework
  Silver (2.2 wt% on silica)
  Surface reaction: 2Agsurf + O2 → 2 AgOsurf @T = 170 °C (no bulk oxidation!)
  msample = 0.5021 g Vpulse = 0.00925 cm3 O2@RT@1atm Max TCD signal = 0.022
  D = ?
Pulse | TCD signal
#1 | 0
#2 | 0
#3 | 0
#4 | 0
#5 | 0
… | …
#28 | 0
#29 | 0
#30 | 0.002
#31 | 0.005
#32 | 0.011
#33 | 0.016
#34 | 0.019
#35 | 0.021
#36 | 0.022

## Slide 46: Chemisorption
Adsorption of IR (NMR) active molecules
  Pyridine and its derivatives
  CO
  Trialkylphosphine oxides
  …

## Slide 47: Chemisorption
Adsorption of IR (NMR) active molecules
  Number of sites
    Lambert-Beer law
  Strength of sites
    Desorption under vacuum at different temperatures
  Nature of sites
    Different vibration modes

## Slide 48: Chemisorption
Adsorption of IR (NMR) active molecules
Example: pyridine adsorption on an acid catalyst

## Slide 49: Chemisorption
Adsorption of IR (NMR) active molecules
Example: CO adsorption on MgO, a catalyst that activates methane for oxidation, ideal products are ethane and ethylene
  2 CH4 + 0.5 02 → C2H6 + H2O
  2 CH4 + 02 → C2H6 + 2 H2O
Mg O Mg O Mg O
Hδ-∙∙∙C δ+H3

## Slide 50: Chemisorption
Example: CO adsorption on MgO

## Slide 51: Chemisorption
Example: CO adsorption on MgO

## Slide 52: Chemisorption
Example: CO adsorption on MgO
Single step edge is the active site
  Good correlation between integral of absorption band at 2147 cm–1 and catalytic activity
  Band at 2147 cm–1 represents single step edge
  Au atoms selectively deposits on single step edges (observed by HR-TEM) = catalyst poisoning, active site „titration“

## Slide 53: ToF-SIMS
Time of flight secondary ion mass spectrometry
Catalyst surface bombarded by „primary“ ions (e.g. Bi5+)
Surface atoms (top ≈1 nm) expelled by this bombardment forming charged clusters = secondary ions created
Analysis of secondary ions gives us information about catalyst surface

## Slide 54: ToF-SIMS
Surface composition
  AlO2– is a function of Al concentration in top 1 nm
  AlSiO3– is a mixed Al-Si cluster (good Al dispersion)
  Al2O4– signifies badly dispersed Al species

## Slide 55: Catalyst characterization
Outline
  DRUV
  XPS
  XANES & EXAFS
  Chemisorption
  ToF-SIMS