## Slide 1: Nonferrous Metals and Alloys (phase diagrams and phase transformations)
Prof. RNDr. Jiří Sopoušek, CSc.
Brno, PS
Audio test:

## Slide 3: Copper alloys
Copper is one of the earliest metals to be used by humans (8500 BC, northern Iraq: Selwyn 2004[1]). Copper alloys are often divided in four large families: pure Cu, bronzes (Cu/Sn), brasses (Cu/Zn) and quaternary alloys (Cu/Sn/Zn/Pb). The oldest Cu alloys contained As or Sb. Zn, Pb or As are often secondary elements in bronzes whereas brasses can contain Sn or Pb. Cu/Ni, Cu/Zn/Ni and Cu/Al alloys have been developed in recent times (19th century).
https://micorr.org/scientific-bases/

## Slide 4: Bronze (Cu+Sn)
Bronze is a 80+% copper alloy and 90+% copper&tin alloy (commonly 12–12.5% tin) with often the addition of other metals, such as aluminium, manganese, nickel or zinc, and sometimes non-metals or metalloids such as arsenic, phosphorus or silicon. These additions produce a range of alloys that may be harder than copper alone, or have other useful properties, such as stiffness, ductility, or machinability.
https://en.wikipedia.org/wiki/Bronze
Typically, pure annealed copper shows a hardness of HV1 40-50. Small additions of Sn or Sb increase this slightly, to HV1 70-100. Cast tin bronzes or alloys with final cold working show the highest hardness values (HV1 between 120 and 180).

## Slide 5: Cu-Sn Phase diagram
As cast, bronzes are categorized as belonging to the Cu α phase only if their Sn content does not exceed 4 mass% (Fig. 2). Above this value the alloys have an α (alpha) + δ (delta) microstructure. Depending on the Sn and secondary elements (Pb, As) content, as well as the heat treatments applied, bronzes are either constituted of Cu α phase or Cu α phase associated to the eutectoid α + δ phase. Pb (up to 7 mass% in the alloys studied) is insoluble in copper alloys and forms inclusions. Their fineness and regular distribution give high quality alloys.

## Slide 6: Structures of phases
https://www.copper.org/resources/properties/microstructure/cu_tin.html
Nominal Composition: Cu 88-90, Sn 10-12, Pb .50, Zn .50, Ni .50, P .30, Sb .20, Fe .15, S .05, Al .005
Bronze microstructure

## Slide 7: Cu-Sn phase transformations

## Slide 8: Brass Cu+(5-40)wt%Zn
Brass is an alloy of copper and zinc, in proportions which can be varied to achieve varying mechanical and electrical properties.[1] It is a substitutional alloy: atoms of the two constituents may replace each other within the same crystal structure.
https://en.wikipedia.org/wiki/Brass

## Slide 10
https://www.kme.com/fileadmin/DOWNLOADCENTER/COPPER%20DIVISON/4%20Industrial%20Rolled/4_Alloys/CuZn36.pdf

## Slide 11: Cu-Sn phase diagram
https://micorr.org/scientific-bases/

## Slide 12: Hardering of Cu alloys
Copper alloys that are hardened through heat treatment are divided into two general types:
those that are softened by high-temperature quenching and hardened by lower-temperature treatments (comprise pure Cu)
and those that are hardened by quenching from high temperatures through martensitic-type reactions.
Alloys that harden during low-to-intermediate temperature treatments following solution quenching include
precipitation hardening,
spinodal-hardening
and order-hardening types.
Quench-hardening alloys comprise aluminum bronzes, nickel-aluminum bronzes, and a few copper-zinc alloys.
http://www.totalmateria.com/Article71.htm

## Slide 13: Al alloys
Aluminium alloys were developed in the later part of the 19th century. Pure aluminium was first produced chemically at a very high cost. When electrolytic production was developed in 1886 the metal became cheap and very quickly found use as an important industrial material. Aluminium alloys are divided in families: Al, Al/Cu, Al/Mn, Al/Si, Al/Mg, Al/Mg/Si, Al/Zn. Some of them are cast, others are wrought alloys hardened by heat treatment (heat-treatable: Al/Cu, Al/Mg/Si and Al/Zn) or by the presence of the alloying elements (non-heat-treatable: Al, Al/Mn, Al/Mg) (Selwyn 2004[1]).

## Slide 14: Al-Cu phase diagram
https://micorr.org/scientific-bases/

## Slide 15: Sn-Pb alloy
Phase diagram of Pb-Sn alloys with sketches of the microstructure observed depending on the composition of the alloy (from http://www.benbest.com/cryonics/lessons.html, accessed on January, 02 2018). The eutectic point corresponds to a mixture of elements having a unique chemical composition that solidifies at a lower temperature than any combination of the same constituent elements.
https://micorr.org/scientific-bases/

## Slide 16: Discussion